P R O D U C T  D A T A  S H E E T

__________________________________________________________

Product: CROSSLINKER					Date: 01/12/2021

Code: M-702R							DOT Class: N/A

B R E A K D O W N:

## Trimethylolpropane tris(2-methyl-1-aziridine propionate)    CAS: 64265-57-2

2-Butoxyethanol                                                                 CAS: 111-76-2

S P E C I F I C A T I O N S:

Wt/gal: 8.1±0.1 lbs/gal

%Solids:

Weight: 49.0±1

Volume: 44.0±1

Theoretical V.O.C.

Lbs/gal: 4.1(less exempt solvent)

Grams/Liter:

Viscosity: N/D

Mixing Ratio: 3 liq.oz/gal

Protect from freezing

C O M M E N T S:

Shelf Life – 1 year unopened containers stored at R.T. 50% R.H.

This Technical Data Sheet is an accurate to the best of our knowledge. However, as applications,

conditions and intended end use are beyond our control, no warranty as to fitness or merchantability is expressed or implied. Customers are urged to confirm their own results.